PRATOPRATICO® - Specifications

Laying of treadable grass flooring with Pratopratico®

Art. 1) PERMEABLE LAYER - Placing of permeable layer underlying the grass treadable flooring, through the supply and laying of crushed stone made of fine, variable, granular pieces 3/10 mm, well spread and rolled by hand, into a finished thickness of about 5/7 cm.

€ per square meter _______________________________________

Art. 2) FLOORING - Supply and laying of two-faced flooring elements such as “Pratopratico®” with the following technical characteristics

• Precious, virgin PP Material (polypropylene) adapted to work with UV rays with mechanical performance characteristics of the highest quality:

• Impact resistant to cold temperatures (-20C) and at least 8Kj/m2 (ISO 180 method) to guarantee the entirety of the flooring even if stressed and placed in extreme environmental conditions;

• Laying capacity of at least 320 t/sq. m (monotonic loading breaking point test);

• Softening point of at least 152°C to guarantee nondeformability of the product in the presence of high temperatures (see flooring filled with crushed stone and placed during the summer season).

• Size in centimetres: 50 x 50 x 5;

• At least 95% grass and permeable surface;

• Reversible: both sides can be used;

• Shaped as in attached design;

• Cell border must be at least 4.7 cm to guarantee a congruous nutritional baggage to the grass and a suitable structure for the exchange of air, water and nutritional elements;

• Male-female joint hooking system; flooring kept still with sealing chamfers;

• Possiblility of laying signalling elements (in white, yellow and blue) to delimit the parking areas and walkways;

Once laid in place, the above-mentioned flooring has technical characteristics that make it immediately suitable for vehicle transit.

€ per square meter _______________________________________

Art. 3) FILLING OF LAWN FLOORING - Laying of lawn surface by filling the Pratopratico® flooring type cells with a blend of excellent vegetable soil, peat, siliceous sand and/or inert volcanic material (pumice) encriched with slow-release fertilizer; Supply and sowing of an excellent blend of seeds for grass suitable for vehicle transit (type: poa pratensis/lolium perennial/festuca arundinacea) in amounts of 35/40 gr. per sq. m. Including any extra charges to provide the final product.

€ per square meter _______________________________________

Art. 4) DELIMITING OF PARKING AREAS AND WALKWAYS - Supply and laying of signalling elements...(in white, yellow and blue) to delimit the parking and/or walkway areas, to be placed in the soil inside the cells of the Pratopratico®, flooring according to the requirements of D.L..

€ per piece _______________________________________

The flooring must be produced by companies with a Quality, Environmental, Safety, and Social Accountability System certified in compliance with International provisions UNI EN ISO 9001, UNI EN ISO 14001, UNI EN ISO 45001, SA8000.

Laying of gravel treadable con surface with Pratopratico®

Art. 1) PERMEABLE LAYER

Placing of permeable layer underlying the treadable gravel flooring, through the supply and laying of crushed stone made of fine, variable, granular pieces 3/10 mm, well spread and rolled by hand, into a finished thickness of about 5/7 cm.

€ per square meter _______________________________________

Art. 2) FLOORING

Supply and laying of two-faced flooring elements such as Pratopratico® with the following technical characteristics:

• Precious virgin PP Material (polypropylene) adapted to work with UV rays with high mechancial performance characteristics of the highest quality:

• Impact resistance to cold temperatures (-20C) and at least 8Kj/m2 (ISO 180 method) to guarantee the entirety of the flooring even if stressed and placed in extreme environmental conditions;

• Laying capacity of at least 340 t/sq. m (permanent loading test);

• Softening point of at least 152°C to guarantee nondeformability of the product in the presence of high temperatures (see flooring filled with crushed stone and placed during the summer season).

• Size in centimetres: 50 x 50 x 5;

• At least 95% grass and permeable surface;

• Reversible: both sides can be used;

• Shaped as in attached design;

• Cell border of at least 4.7 cm;

• Male-female joint hooking system; flooring kept still with sealing chamfers;

• Possiblility of laying signalling elements (in white, yellow and blue) to delimit the parking areas and walkways;

Once laid in place, the above-mentioned flooring has technical characteristics that make it immediately suitable for vehicle transit.

€ per square meter _______________________________________

Art. 3) FLOORING FILLING WITH FINE GRAVEL

Laying of gravel flooring by filling the cells with Pratopratico® type flooring with fine gravel (granes of 7/10 mm).

€ per square meter _______________________________________

Art. 4) DELIMITING OF PARKING AREAS AND WALKWAYS - Supply and laying of signalling elements...(in white, yellow and blue) to delimit the parking and/or walkway areas, to be placed in the soil inside the cells of the Pratopratico®, flooring according to the requirements of D.L..

€ per piece _______________________________________

The flooring must be produced by companies with a Quality, Environmental, Safety, and Social Accountability System certified in compliance with International provisions UNI EN ISO 9001, UNI EN ISO 14001, UNI EN ISO 45001, SA8000.