E.C.O. by Pratopratico® - Specifications

1. Placing of permeable layer underlying the grass driveway flooring through the supply and lying of crushed stone made of fine, variable, granular pieces 3/10mm, well spread and rolled by hand, into a finished thickness of about 5/7 cm.

€ per square meter _______________________________________

2. Supply and laying of the flooring elements such as E.C.O. of Daliform Group srl with the following technical characteristics:

• 50% recycled and 50% virgin PP material (polypropylene) with impact resistant to cold temperatures (-20°C) and at least 8 kJ/m2 and to hot temperatures (+23°C) about 40 kJ/m2 (ISO 180 method); softening point of at least 152°C (ISO 306/A method) and UV rays resistant;

• Laying capacity of at least 300 t/m2 (monotonic loading breaking point test);

• At least 95% grass and permeable surface;

• Soil volume: not less than 165 cm³ for every single grating;

• Male/female joint hooking system; flooring kept still with sealing chamfers;

• Possibility of laying signalling elements (in white, yellow and blue) to delimit the parking areas and walkways;

Once laid in place, the above-mentioned flooring has technical characteristics that make it immediately suitable for vehicle transit.

€ per square meter _______________________________________

3. Laying of lawn surface by filling the E.C.O. flooring type cells with a blend of excellent vegetable soil, peat, siliceous sand and/or inert volcanic material enriched with slow-release fertilizer; supply and sowing of an excellent blend of seeds for grass suitable for vehicle transit in amounts of 35/40 gr per sq. m.

€ per square meter _______________________________________

4. Supply and laying of signalling elements in white, yellow and blue to delimit the parking and/or walkway areas, to be placed in the soil, inside the cells of the E.C.O. flooring according to the requirements of D.LL.

€ per square meter _______________________________________

The flooring must be produced by companies with a Quality, Environmental, Safety, and Social Accountability System certified in compliance with International provisions UNI EN ISO 9001, UNI EN ISO 14001, UNI EN ISO 45001, SA8000.