Specifications

SISTEMA ATLANTIS

Implementation of a ventilated under-ground cavity for a total height of  ______ cm with the supply and on-site positioning of recycled plastic Atlantis System formworks from the Daliform Group, consisting of modular formworks positioned dry for the quick dry formation of a self-bearing pedestrian accessible platform above which the C25/30 concrete is cast to fill the formwork up to its crown and an upper slab of ______ cm reinforced with welded mesh Ø ______ cm ___ x ___ cm, levelled and smoothed with a trowel.

The Atlantis system 50 shall be composed of recycled plastic formwork such as Iglù® with convex cover with dimensions 50x50 cm, h 16 cm and sustained by pipes Ø110 mm, di h ______ cm, complete with slip on bayonet connection feet, which can be walked on when dry, guaranteeing a breaking resistance of 200 kg in correspondence of the centre of the arch with an 8 x 8 cm clamp.

or

The Atlantis 71 system shall be composed of recycled plastic formwork such as Iglù® with convex cover with dimensions 71x71 cm, h 15 cm and sustained by pipes Ø110 (or Ø125, or Ø140) mm, di h ______ cm, complete with slip on bayonet connection feet, which can be walked on when dry, guaranteeing a breaking resistance of 150 kg in correspondence of the centre of the arch with an 8 x 8 cm clamp.

or

The Atlantis 100 system shall be composed of recycled plastic formwork such as Iglù® with convex cover with dimensions 100x100 cm, h 12 cm and sustained by pipes Ø110 (or Ø160) mm, di h ______ cm, complete with slip on bayonet connection feet, which can be walked on when dry, guaranteeing a breaking resistance of 200 kg in correspondence of the centre of the arch with an 8 x 8 cm clamp.

Atlantis system will be equipped with the corresponding accessories, such as “Tympanum”, “Shelf” and “Angle” for the lateral occlusion and compensation, to be calculated and quantified according to the conformation of the area.

Formworks in recycled plastic, such as Iglù®, for the formation of the Atlantis system, must not release polluting substances, have an Environmental Compatibility Certification and be produced by a Company Certified according to International Standards UNI EN ISO 9001 (Quality), UNI EN ISO 14001 (Environment); UNI EN ISO 45001 (Safety) and SA 8000 (Social responsibility).

The company that supplies the formworks such as Iglù®, for the formation of the Atlantis system ,must also exhibit the product certificate approved by an EOTA (European Organisation for Technical Approvals) member agency.

Including accessories, waste, cutting and all other expenses: ______  /m2 ______