U-BOOT SILENCE® SPECIFICATIONS

Implementation of sound insulation of slabs such as "U-Boot Beton®" from noise of footsteps and airborne, made with the technique of the "floating floor" through the use of the sound insulation mantle "U-Boot Silence" by Daliform Group made, of 100% closed cell polyolefin chemical cross-linked polyethylene, density 35 kg/m3, thickness 8 mm, low elastic module, color yellow The product comes in rolls of H 1.5 m x L 60 m. The installation must be performed aligning the heads of the side flaps and sealing of joints by applying the adhesive strip “Rotocell AD”. The surface must be perfectly superimposed to the appropriate perimeter buffering "Superfascia AD." The layer on which to lay the product must be perfectly dry, clean and free of bumps.

On top of the insulation layer is laid a concrete screed, at least 4 cm thick, on which will then be made the flooring planned. The excess of insulating material present along the perimeter will be trimmed only once the  floor is finished, masked by the application of the baseboard, which will be detached from the floor in order not to determine "sound transmission".